## Slide 1: Meeting with Nuvia
Saad Shaikh, Sonia Escribano-Rodriguez1, Raffaella Radogna, Connor Godden, Derek Attree, Samuel Manger, Karen Kirkby, Marc-Jan Van Goethem, Alexander Gerbershagen, Simon Jolly
1sonia.escribano@ucl.ac.uk
DEPARTMENT OF PHYSICS AND ASTRONOMY
2nd November 2023, London

## Slide 2
Sheet thickness should be 3.0mm.

## Slide 4
Experiment 16th June 2022
2
Sheets were 3.4mm thick instead of 3mm. Due to PD separation the sheets had to be compensated with a 2mm thick sheet every two.

## Slide 5
Cross-talk measurements
2
Thickness of the sheets really affects the light cross-talk
Rev B: 0.78% cross-talk
Rev C: 2 thick + 1 thin -> 5.11% cross-talk

## Slide 6
Fit Results
2
The increase in cross-talk light leads to inconsistent fits
Rev B
Rev C

## Slide 7
Experiment 1st September 2022
2
Correct thickness, but light output lower than expected: about 40% down on the set of sheets that average 2.86mm. It also looks like there is a fair amount of variation in light output between sheets.

## Slide 8
Shoot through comparisons
1
Rev. C Clear Polished
(misaligned photodiodes)
Rev. D Clear Opaque
Rev. B Clear Polished
Rev. B White Painted
Rev. B Black Painted
Rev. C Clear Polished
(misaligned photodiodes)
Rev. D Clear Opaque
Rev. B Clear Polished
Rev. B Clear Polished & White Painted
Light comparisons