Report on the testing of the proposed ATLAS Inner Detector barrel thermal enclosure bulkhead services, grommets and proposed sealant.

| Author(s) | ### B. E. Anderson, D. J. Attree, T. J. Fraser. |
| --- | --- |

| ### Document number | ATLAS SCT UCL grom001 |
| --- | --- |
| Document status | For discussion |

| ### Issue date | 23.04.2001 | Issue number | 6 |
| --- | --- | --- | --- |
| #### Revision dates |  | #### Revision number |  |
| 22.05.2001 |  | 1.1 |  |
| 28.02.2002 |  | 1.2 |  |
| 03.06.2003 |  | 1.3 |  |
| 17.06.2003 |  | 1.4 |  |
| 11.09.2003 |  | 1.5 |  |

Related documents.

ATLAS SCT UCL  grom002

Report on the testing of the proposed ATLAS Inner Detector barrel optical fibre splice cover tubes.

### ATLAS SCT UCL  grom003

Report on the testing of the adhesion of aluminium foil to the ATLAS SCT barrel thermal enclosure Kapton-aluminium heating film and a peel strength test of a pressure-sensitive tape.

ATLAS SCT UCL  grom004

Report on the determination of the density and viscosity of Techsil 6166 + 50% talc, and calculations and tests on application methods.

Contents.

Apologies are given for the somewhat inchoate listing below, but the test programme grew organically as new requirements became obvious and various tests failed to meet specification.

1. Scope of document.

2. Purpose of tests.

3. Leak testing of silicone rubber grommets for the low mass power tapes.

3.1 Apparatus and assembly techniques for leak testing.

3.2 The leak test results.

3.3 Radiation testing the plate.

4. Testing the extension under load of the power tape grommet flange and an EPDM sample

4.1 Test apparatus.

4.2 Elasticity test results.

5. Inducing failure in the power tape sealing mechanism.

5.1 Flexing the power tapes within the seal.

5.2 Testing the seal under axial load.

5.3 Bond strength of Techsil 6166 + 50% talc with silicone rubber and Kapton adherends.

5.4 Bond strength of Techsil 6166 + 50% talc with EPDM and Kapton adherends.

5.5 Modulus of elasticity (Young’s modulus) and tensile strength of Techsil 6166 + 50% talc.

6. Tests on the furcation tubing.

7. Adhesion tests on polyetheretherketone (PEEK)

7.1 PEEK: Techsil 6166 50% talc loaded:Kapton low mass power tape

7.2 PEEK: Techsil 6166 50% talc loaded: F00fR900R3L furcation tubing.

7.3 PEEK: Techsil 6166 50% talc loaded: Optical fibre ribbon S-12T-50/60/125-R.

8. Load tests on Stycast 2741.

9. Adhesion tests on Stycast 2741.

10. Testing the efficacy of Techsil mastic as sealant for the aluminium alloy mating surfaces of the bulkhead.

11. Leak testing a PEEK grommet containing 6 Kapton-aluminium power tapes and Techsil 6166 + 50 per cent talc.

11.1 Test results.

12. Adhesion test of DCS wires to PEEK using Techsil 6166 + 50% talc.

13. Leak testing a PEEK grommet containing 72 F00fR900R3L furcation tubes and Techsil 6166 + 50 per cent talc.

14. Thermal tests on Techsil 6166 + 50% talc.

13.1 Coefficient of thermal expansion.

13.2 Change in elasticity with temperature.

15. Retesting irradiated components and materials.

15.1 Stycast 2714/catalyst 15.

15.1.1 Hardness tests.

15.1.2 Modulus of elasticity.

15.2 Furcation tubing.

15.3 EPDM.

1. Scope of document.

This document describes

- the leak tests conducted on the various grommets and grommet materials that allow the services to pass through the ATLAS thermal enclosure envelope,

- tests to determine the extension under load and the adhesive bond strength of the various components and materials,

- tests of the strength and elasticity of the proposed sealant.

2. Purpose of tests.

To determine the leak rate of the various proposed methods of leak sealing the grommet and services, to test the elasticity of the proposed materials and to test the elasticity, bond strength and tensile strength of the proposed sealant.

3. Leak testing of silicone rubber grommets for the low mass power tapes.

3.1 Apparatus and assembly techniques for leak testing.

The grommets are based on RAL drawing number A2-TB-0049-155-00-A  (Feedthough sleeve [SCT] [Inner detector services]) but were fabricated (rather than moulded) from silicone rubber sheet. Four of the grommets were each mounted with a group of six power tape segments and sealed with a mixture of Techsil 6166 RTV silicone rubber and BDH fine talc (magnesium silicate hydroxide: Mg3Si4O10(OH2)) in the ratio 10:5. A schematic of the assembly is given in Figure 1.

Slotted aluminium alloy test plate

Power tape

RTV

Grommet

sealant

Figure 1. Power tapes and grommet shown mounted through alloy plate with RTV sealant.

The power tapes were cleaned with ethanol and then glued together in groups of six by spreading a small amount of RTV sealant on the tape surfaces and then stacking and loading with a 1kg weight and leaving the RTV sealant to cure for 16 hours. Care was taken to ensure that the tapes were aligned accurately within their respective groups. The slotted test plate and grommets were cleaned with ethanol and the groups of tapes passed through the grommets. A bead of RTV sealant was run around each slot in the test plate and the grommet-power tape assemblies fitted to the slots. RTV sealant was then added as shown in Figure 1, ensuring that all potential gaps were filled or covered with RTV sealant. The RTV sealant was applied using thin wooden spatulas cut from cotton bud sticks. This assembly was then allowed to cure for 16 hours

Test plate with 4 x 6 power tape segments

Manometer

Test box

N2 supply

Figure 2. The test apparatus for leak-testing the grommet-power tape assemblies.

Before the test plate with the power tapes was tested, the box was qualified using an unslotted plate with the same external dimensions as the test plate. This test methodology is essentially the same as that described in versions 1.0 and 1.1 of this document, using the apparatus shown in figure 2. However, the following changes were made to the procedure:

- the amount of talc was reduced from 10 parts Techsil : 8 parts talc to 10 parts Techsil : 5 parts talc (described below as Techsil + 50% talc) in order to improve the applicability and wetting while maintaining a sufficient viscosity to avoid excessive slumping or run-off,

- the water in the manometer was replaced with a low vapour pressure silicone oil,

- the overpressure inside the box was raised from 5.5 to 10 hPa (1hPa = 1mbar),

- the test period was extended from around 4 to 720 hours (30 days),

- as a result of which corrections had to be made to allow for changes in temperature and barometric pressure.

3.2 The leak test results.

### Figure 3 shows the net pressure drop over a 720-hour period. There is a net pressure drop over the period of about 1.3 hPa, giving a leak rate of 3.1 x 10-4   l.hPa-1.hr-1. (Note: the box has a volume of 4.5l). The error bars are dominated by the precision of the digital barometer (± 1 hPa).

Figure 3. Overpressure vs. time results for the test box with the test plate plus 4 x 6 power tape assemblies.

Note that for the full set of power tapes from all barrels, the inferred leak rate will be 1.6 x 10 -3 l.hPa-1.hr-1, assuming there are 12 (not 6) tapes per grommet.

3.3 Radiation testing the plate.

Arrangement were made to irradiate the plate under conditions assumed to be similar to those that would be experienced in ATLAS. The plate was exposed to a flux of 300 kGy of gamma radiation over five days. After that the plate was retested using the same procedure as above. The plot of pressure drop with time is given in Figure 3a, with the original plot shown for comparison.

Figure 3a. Overpressure vs. time results for the test box with the test plate plus 4 x 6 power tape assemblies – pre and post radiation testing.

### It can be seen that there is little variation between the slopes. We concluded that the assembly of Techsil, grommet and tapes had survived the test undamaged. This conclusion was reached, however, without subjecting any element to mechanical stress. The result was not entirely expected as will be shown below.

4. Testing the extension under load of the power tape grommet flange and an EPDM sample.

There was a possibility that the material of the grommet might harden as a result of irradiation. We decided to test the elasticity of the grommet material to determine whether any hardening was detectable after irradiation. This initial test measures the elasticity before the sample is irradiated. The grommet flange was chosen as the test subject because it is flat (unlike the sleeve or the complete grommet) and therefore less likely to distort in planes non-parallel to the direction of the applied load.

4.1 Test apparatus.

The apparatus is shown in Figure 4. Essentially, the equipment consists of a pair of carefully machined clips that allows the flange to be held in a repeatable position while the measurements are taken, an upper support, a scale pan and a vernier height gauge to measure the extension. It is, in effect, an apparatus to test Hooke’s Law.

Grommet flange

Height gauge

Surface plate

Figure 4. Apparatus for testing grommet flange extension under load.

4.2  Elasticity test results

These are shown in Figure 5. The extension vs. load curve is essentially linear.

Figure 5. Load vs. extension plot of grommet flange

We allowed the sample to relax after loading and measured the length again. We found that it had returned to its original dimension, indicating that it had not been loaded to the elastic limit.

The post-irradiation test proved to be redundant as the sample (irradiated in the same box as the 4-tape plate) disintegrated on removal. Since this discovery, EPDM (ethylene propylene diene monomer) has been proposed as an alternative grommet material. A similar Hooke’s Law test has been conducted, as shown in Figure 6.

Figure 6. Hooke’s Law test on EPDM strip.

5. Inducing failure in the power tape sealing mechanism.

Although the leak testing described in section 3 allows considerable confidence in the sealing method, we considered the possibility that stresses on the power tapes during installation (especially high force traumatic incidents) might cause the seal to fail. We therefore conducted a series of tests designed to challenge the robustness of the seal.

5.1 Flexing the power tapes within the seal.

We manufactured another slotted test plate with only one slot and mounted a grommet and 6 power tapes in a manner similar to the one described in section 3. The tapes were flexed by 90º in a direction normal to the plane (test axis A) of the tapes and by about 5º in a direction parallel to the plane (test axis B) (the deviation of the tapes in this direction was limited by the fairly small clearance between the tape bundle and the internal surface of the grommet and slot).

This is shown schematically in Figure 7.

Test plate with grommet, RTV and 6 power tapes

Test axis A

Test axis B

Figure 7. Test arrangement for power tape flexing

We pressurised the test box to 10 hPa overpressure and flexed the tapes close to the grommet, firstly on axis A at ±10º intervals (with a relaxation at θ = 0º after each reading and to limits of ± 90º), then on axis B at very approximately 1º intervals with a similar relaxation. About 5 minutes was allowed for each position. The whole test series lasted about 90 minutes.

At no point did we observe a pressure drop, indicating that the seal integrity and elasticity of the RTV sealant is sufficient to withstand “normal” power tape handling.

5.2 Testing the seal under axial load.

We considered this test to be representative of the kind of load that the power tapes and seal might experience if they were suddenly tugged.

The tape arrangement described in section 5.1 was repeated and the box again pressurised to 10 hPa.

A strong relatively inflexible line was attached to the power tape bundle via a hole drilled through the set as shown in Figure 8. The load was gradually increased in 10g wt intervals from 0 to 120g wt (1.17N), then in 50g wt intervals to 400g wt (3.9N). About 10 minutes were allowed between loadings. Until 300g wt there was absolutely no detectable movement of the tapes or distortion of the seal. At 350g wt, there was a discernible stretch in the seal, although the assembly remained stable. At 400g wt, the RTV sealant began to tear and the seal failed after 35 minutes.

The test was then repeated the following day (by cleaning off the residue of sealant from the original test and then re-gluing) with a 300g wt (2.9N) load and the assembly carefully watched for changes. Table 1 shows the changes observed.

Inside of box

(10 hPa)

Point A

Figure 8. Test arrangement for axially loading the tape bundle and seal

| Elapsed time (minutes) | Observed changes | Box overpressure (hPa) |
| --- | --- | --- |
| 0 | No change | 10 |
| 10 | No change | 10 |
| 20 | No change | 10 |
| 30 | No change | 10 |
| 45 | No change | 10 |
| 52 | Tear in RTV sealant at point A | 10 |
| 85 | Tape bundle slipped through grommet by 5mm. Tear now extensive | 10 |
| 87 | Tape bundle slipped by 10mm | 8.3 |
| 90 | Tape bundle slipped by 15mm | 6.9 |
| 93 | Failed | 0 |

Table 1. Observed changes with 6-tape bundle and seal under axial load of 2.9 N

When we examined the tape bundle, it seemed that the failure was primarily caused by the weakness of the adhesive bond between the polyimide of the power tape and the RTV. There was, however, enough uncertainty about the failure mode to prompt a further series of tests.

5.3 Bond strength of Techsil 6166 + 50% talc with silicone rubber and Kapton adherends.

We conducted two essentially similar tests. Firstly bonding two power tapes together and testing the bond strength to failure, then doing a similar test bonding a power tape to silicone rubber (RS 246-1659). Figure 9 shows the test arrangement. Figures 9a and 9b show the test results. The bond area was 40 x 21 mm in each case and the RTV thickness around 0.2mm. 5 minutes were allowed between each increase in load.

Test sample

Figure 9. Test arrangement for bond testing Techsil 6166 + 50% talc for two adherends.

Figure 10a. Bond strength of Kapton-to-Kapton.

Figure 10b. Bond strength of Kapton-to-silicone rubber.

In the case of Figure 10a, we conducted an independent series of measurements on the silicone rubber alone, which allowed us to subtract the effect of its elasticity from the test.

It is clear from the plots at Figures 10a and b that the bond strength in the case of silicone rubber-to-Kapton (failure at approx. 1200 g wt, 11.8N) is more than twice as great as for Kapton-to-Kapton (failure at approx. 500 g wt, 4.9N). Since Kapton is often very difficult to bond to without preparation unacceptable to the electrical breakdown integrity of the power tapes, it is unsurprising that the failure occurs at a much lower load when two Kapton surfaces are involved compared with just one.

5.4 Bond strength of Techsil 6166 + 50% talc with EPDM and Kapton adherends.

A similar test to those described above was conducted with EPDM and a section of low mass power tape. The result is shown in Figure 11 below. It was observed that, after the Techsil curing period, an oily residue had spread from the bond area. This presumed to be a product of reaction between the EPDM (or possibly plasticiser) and the Techsil. Adhesion testing led to failure of the bond (if any) at less than 0.24N, suggesting that the surface tension of the leachate was the only thing holding the sample together. A repeat test using much more aggressive cleaning of the EPDM prior to bonding gave the same result.

5.5 Modulus of elasticity  (Young’s modulus) and tensile strength of Techsil 6166 + 50% talc.

We designed this test to gather some idea of the elasticity and bulk strength of the sealant.  We made a PTFE mould that allowed us to cast a strip of the sealant 50 x 11 x 2.5 mm. The sealant strip was left to cure for 16 hours before being removed from the mould. The sample was secured to the apparatus by gluing four small strips of glass-reinforced epoxy to the ends with unfilled Techsil. This gluing operation was done without loading the glue joint (in order to preserve the profile of the strip) and was also left for 16 hours. We then measured the extension with increasing load to a precision of 0.2mm.  The sample was allowed to relax back to its unloaded position after loads of 5, 15 and 25g had been applied. There was no discernible plastic deformation. The apparatus and test arrangement is shown at Figure 11 and the resulting curve at Figure 12.

Test sample of filled Techsil

G10 fixtures

23mm

Figure 11. Measurement arrangement for the tensile strength and modulus of elasticity of Techsil 6166 RTV sealant + 50% talc

Figure 12. Results of the tests on the elasticity and strength of 50% talc-loaded Techsil 6166

The test results allowed us to determine both the modulus of elasticity and the tensile strength of the material. Table 2 shows the results:

| Modulus of elasticity [Y = (F/A)/(e/L)] | 1.75 x 10-5 GPa |
| --- | --- |
| Tensile strength | 1.38 x 10-2 MPa |
| Elongation at break | ~100% |

Table 2. Derived parameters for filled Techsil

It can be seen that the material has impressive elongation properties but is very weak.

6. Tests on the furcation tubing.

The furcation tubing (type F00fR900R3L) was tested for elasticity using techniques described in section 4.2. Figure 13 shows the resulting curve.

Figure 13. Load tests on furcation tubing

The derived modulus of elasticity is 58 MPa. It is intended to irradiate the sample and remeasure this parameter for change.

An adhesion test onto EPDM using 50% talc-loaded Techsil 6166 failed at an even lower load than that described in section 5.4, and probably for the same reason.

7. Adhesion tests on polyetheretherketone (PEEK)

7.1 PEEK:Techsil 6166 50% talc loaded:Kapton low mass power tape

The test arrangement was as described in section 5.3 and shown in Figure 9. The bond area was 21mm x 45mm and the Techsil thickness about 0.5mm. The load was steadily increased over 14 increments to 1028g-wt (10.1N) at which point the bond failed completely. There was no discernible stretching of the bond (as was seen in Figures 10a and 10b) before failure. Note that the failure load is similar to that shown for silicone rubber and Kapton as shown in Figure 10b.

7.2 PEEK: Techsil 6166 50% talc loaded: F00fR900R3L furcation tubing.

This test is similar to that above except that the tubing was effectively potted in a bead of Techsil on the PEEK surface. The inferred bond area was 34.6 mm2. In this case the load sufficient to cause the tube to slide out of the Techsil was very low – about 1N.

7.3 PEEK: Techsil 6166 50% talc loaded: Optical fibre ribbon S-12T-50/60/125-R.

This test arrangement is as given in the previous sections but using optical fibre ribbon. The bond area was 71.5mm x 3.0mm. In this case the bond sheared at a load of 338.3g-wt (3.3N). There was no discernible stretching of the bond before failure.

8. Load tests on Stycast 2741

Stycast 2751 is an epoxy resin with a variable elasticity depending on the resin: catalyst ratio with Catalyst 15. In this first test we mixed resin to catalyst 1:1.5, giving a flexible product after cure. A thin strip was cut and tested as in section 4. The resultant graph is given in Figure 14.

Figure 14. Load test on Stycast flexible mix.

The modulus of elasticity derived from the graph is 0.52 MPa.

9. Adhesion tests on Stycast 2741/Catalyst 15

We mixed three different ratios resin to catalyst as given in the data sheet. Table 3 gives the details:

| Stycast 2741 proportion | Catalyst 15 proportion | Data sheet description | Local label |
| --- | --- | --- | --- |
| 1 | 1.5 | Flexible | F |
| 1 | 1 | Semi-rigid | SR |
| 1 | 0.5 | Rigid | R |

Table 3. Mix ratios and description of Stycast samples.

We bonded the samples to strips of Kapton-aluminium power tape using Techsil 6166 RTV silicone rubber and talc in the ratio 10:5 and then tested them as described in section 5.3. Table 4 shows the results.

| Stycast mix type | Load at failure | Bond area (mm2) | Comment |
| --- | --- | --- | --- |
| R | 261g wt (=2.6N) | 400 | See Fig. 15 |
| SR | 73 g wt (=0.7N) | 400 | Both samples seemed to have a residue of catalyst, which prevented the Techsil from curing at the interface. |
| F | 39 g wt (=0.4N) | 210 |  |

Table 4. Load test of Stycast vs. Kapton power tape

Figure 15: Adhesion test of Stycast 2741/catalyst 15 (1:1.5) to Kapton low

mass power tape using Techsil 6166 + 50 per cent talc.

10. Testing the efficacy of Techsil mastic as sealant for the aluminium alloy mating surfaces of the bulkhead.

Using the test box described in section 3, we made a pair of chamfered plates that would tightly butt together when bolted to the box. The butting edges each had an area of 6 x 90mm with a 0.25 chamfer on the upper (low pressure) edge. We cleaned these two surfaces and painted with Techsil 6166 + 50 per cent talc. The two plates were then bolted to the box, ensuring a tight location between the surfaces. A secondary bead of mastic was then run along the chamfer. We allowed the whole assembly to cure for 24 hours. Figure 16 shows the schematic arrangement.

Chamfered plates

Sectional view

Figure 16. Schematic of  plate arrangement for Al alloy : Al alloy sealing test

We assumed for this test that the survival time of the seal was inversely proportional to the overpressure as the components under test were rigid and all gaps minimal

On this basis we pressurised the box with dry nitrogen to an overpressure of 2 bar  and monitored the pressure change over 10 days. No leak developed (to a precision of 100 hPa) so we are confident that, properly applied, the Techsil seal should, at the planned operating overpressure of 5 hPa, remain hermetically intact for several years.

We increased the pressure steadily over about an hour and the seal finally ruptured at an over pressure of 5 bar.

11. Leak testing a PEEK grommet containing 6 Kapton-aluminium power tapes and Techsil 6166 + 50 per cent talc.

This test was effectively a repeat of that described in sections 3.1 and 3.2. The same plate was used but a grommet made from PEEK replaced one of the silicone rubber grommet assemblies. The fact that PEEK is rigid meant that we had to manufacture the grommet in two halves and assemble it in situ within the slot in the plate. Figure 16 shows a schematic of the assembled grommet.

Grommet manufactured in two parts and assembled and glued around services (fibres or power tapes)

Figure 17. Schematic of PEEK grommet.

11.1 Test results.

Figure 18 shows the pressure drop with time.

Figure 18. Overpressure vs. time results for the test box with the test plate plus 4 x 6 power tape assemblies (3 silicone rubber, 1 PEEK).

The result is, compared with those obtained in sections 3.1 and 3.2, rather surprising. There is, within the accuracy of the measurements, a smaller leak over the recording period than that obtained with all silicone rubber grommets.

The leak measured represents a pressure drop of 7 x 10-4 hPa-hr-1, from which we infer a leak rate of around 5 x 10 -4 l.hPa-1.hr-1 for all power tapes on all barrels. The only explanation we can offer is that the one silicone rubber grommet we removed had a leak representing just over half the leakage of the whole system. The only other differences over the previous tests arise from a period of very hot weather, which produced discernible changes in the volume and vapour pressure of the oil in the manometer. However, these have been measured and allowed for.

12. Adhesion test of DCS wires to PEEK using Techsil 6166 + 50% talc.

The DCS wires are twisted pair cables with an insulating sleeve over the conductive cores, which seems to be both wrapped helically and fused to the core (the leads were examined under x40 magnification). One wire is sleeved in brown, the other red. We tested the adhesion for each type of insulation using the method described in section 7.2. In both cases the bond failed at about 0.4N.

13. Leak testing a PEEK grommet containing 72 F00fR900R3L furcation tubes and Techsil 6166 + 50 per cent talc.

This test is similar to those carried out on the power tapes (Sections 3 and 10). However, the aluminium alloy plate had only a single slot and the grommet was larger. The size was determined from a tentative scheme designed by RAL that showed that 72 tubes could fit, using hexagonal close packing, into a rectangular slot 22.2 x 4.138mm. Allowing for 0.2mm of filled Techsil between adjacent fibres (Section 5.3), we made the interior grommet slot 24.0 x 4.8mm. The grommet was in two parts, similar to Figure 17. The 72 furcation tubes were cut and sealed into the slot using filled Techsil. In order to prevent leakage, one end of the resulting bundle was immersed in unfilled Techsil in a potting tray in order to cast a gas-tight block.

We then mounted the plate onto the test box and increased the internal pressure to about 10 hPa. As before, the system was left for > 24 hours to allow it to stabilise.

Figure 19 shows schematically the arrangement of grommet, plate, tubes and sealant.

PEEK grommet

Furcation tubes

Box lid

Filled Techsil

Potting tray with unfilled Techsil

Exterior of box

Interior of box

Figure 19. End view of PEEK grommet mounted in test plate showing furcation tubes and sealing of tube ends.

14. Thermal tests on Techsil 6166 + 50%  talc.

14.1 Coefficient of thermal expansion.

This was measured by casting a long strip of the sealant and measuring the change in length over a temperature excursion between +26.4ºC and –4.9ºC. This proved quite difficult as the sealant is very elastic and dimensional changes awkward to measure. We conclude that the CTE is (30 ± 5) x 10 -6 ºC-1. This is slightly greater than the CTE of the aluminium alloy forming the bulkhead but the sealant is so elastic this difference should cause no problems.

14.2 Change in elasticity with temperature.

We assessed this qualitatively during the test above. The sealant was still very elastic at –4.9ºC.

15. Retesting irradiated components and materials.

All samples mentioned below were irradiated with 100kGy (10Mrad) of gamma radiation over a few days before being retested.

15.1 Stycast 2741/catalyst 15.

Table 4 (copied from Table 3) shows the three forms prepared for irradiation. The R and SR forms were too stiff for a modulus of elasticity to be measured, so a (fairly crude) hardness test was devised. The F form was tested as shown in Section 8.

| Stycast 2741 proportion | Catalyst 15 proportion | Data sheet description | Local label |
| --- | --- | --- | --- |
| 1 | 1.5 | Flexible | F |
| 1 | 1 | Semi-rigid | SR |
| 1 | 0.5 | Rigid | R |

Table 4. Mix ratios and description of Stycast samples.

15.1.1 Hardness tests.

We used a 4mm diameter bearing ball loaded vertically with 20kg.wt (1962N), and measured the diameter of the indentation made in each sample. New indentations were made after irradiation. Table 5 gives the results.

| Sample type | Indentation diameter before irradiation (mm) | Indentation diameter after irradiation (mm) |
| --- | --- | --- |
| SR | 4.5 ± 0.1 | 4.4 ± 0.1 |
| R | 6.5 ± 0.1 | 6.6 ± 0.1 |

Table 5. Results on hardness tests.

There is, within the errors, no change to either sample.

15.1.2 Modulus of elasticity.

The modulus of elasticity was measured as shown in Section 8. The results before and after irradiation are given in Table 6.

| Modulus of elasticity before irradiation (MPa) | Modulus of elasticity after irradiation (MPa) |
| --- | --- |
| 0.52 ± 0.04 | 0.46 ± 0.04 |

Table 6. Change in the modulus of elasticity of Stycast sample F after irradiation.

The errors are largely caused by our inability precisely to determine the cross-sectional area – the cross-section varied along the casting. Within the errors, there is no discernible change in the elasticity.

15.2 Furcation tubing.

This was retested as in Section 6. The results are given in Table 7.

| Modulus of elasticity before irradiation (MPa) | Modulus of elasticity after irradiation (MPa) |
| --- | --- |
| 56.8 | 65.6 |

Table 7. Change in the modulus of elasticity of furcation tubing after irradiation.

The change is outside the experimental error of ± 0.5 MPa but the change is relatively small and certainly cannot be detected by “qualitative” handling.

15.3 EPDM.

Section 4.1 describes the original elasticity tests. Table 8 shows the change in the modulus of elasticity after irradiation.

| Modulus of elasticity before irradiation (MPa) | Modulus of elasticity after irradiation (MPa) |
| --- | --- |
| 3.9 | 6.2 |

Table 8. Change in the modulus of elasticity of EPDM strip after irradiation.

Again, there is a measurable change, but the material remains elastic and should be a suitable candidate for the major seals of the TE.

All the following sections are under revision

XXX. Discussion

XX Comments on the test results.

XX  Recommendations.